Dry Cells (Batteries)

Reasons for using dry cells

- Inconvenience caused by the simple chemical cells.

- Unsteady voltage

Primary Cell ( not rechargeable (不可再充電的)

e.g.	zinc-carbon cell, alkaline manganese cell, silver oxide cell

Secondary Cell ( rechargeable (可再充電的)

e.g.	nickel-cadmium cell

Zinc-Carbon Cell

Anode (		,		,				)

Eq.

Cathode (			,		,				)

Eq.

They hydrogen formed has to be removed, because

1.

2.

Function of carbon

Function of manganese(IV) oxide

Eq.

Overall Eq.

After discharging

1.

2.

3.

Q:	Why does the cell leak after a certain period even if no current is drawn from the cell?

A:	Since NH4Cl is acidic, it reacts with Zn: Zn(s) + 2H+(aq) ( Zn2+(aq) + H2(g)

The zinc case becomes thinner and leakage eventually occurs.

Prevention of leakage ( coat a stainless steel layer on the batteries

Reasons for choosing dry cells

Price*

Size

Uses

Voltage required

#Candidates are required to select the correct type of dry cells with reasons.

# Calculation

Given

| Brand | A | B | C | D |
| --- | --- | --- | --- | --- |
| Price per battery / $ | 1.5 | 2.5 | 3.5 | 5.0 |
| Average life when using on a walkman / hr | 6 | 7 | 8 | 18 |
| No. of flashes that can be produced when using on a flashlight | 10 | 20 | 25 | 60 |

Calculate

| Brand | A | B | C | D |
| --- | --- | --- | --- | --- |
| Price per hour of service when using on Walkman |  |  |  |  |
| Price per flash when using on a flashlight |  |  |  |  |

Which battery is

- most likely an alkaline battery

- the best buy for using in the Walkman

- the best buy for using in the flashlight

Pollution

Dry cells usually contain a small amount of mercury* (mercury and its compounds are highly toxic to both human beings and aquatic lives)

*Mercury is used to prevent the formation of hydrogen in the cell during storage.

For rechargeable cells, they usually contain extremely toxic cadmium.

# Exercise 1

The following diagram shows the longitudinal structure of a silver oxide cell.

The half-equations for the reactions occurred at electrodes A and B during discharge are

Zn(s) + 2OH-(aq) ( ZnO(s) + H2O(l) +2e-

Ag2O(s) + H2O(l) +2e- ( 2Ag(s) +2OH-(aq)

- Which electrode, A or B, is the anode? Explain your answer.

- Write the overall equation for the reaction that would occur in the cell during discharge.

- Unlike zinc-carbon cell, silver oxide cell does not leak readily. Suggest a reason.

- Explain why silver oxide cells are only used in small devices such as watch and calculator.

- If the silver oxide in electrode B is replaced by mercury (II) oxide, the cell becomes a mercury oxide cell. The half equation occurred at electrode B becomes: HgO(s) + H2O(l) + 2e-  ( Hg(l) + 2OH-(aq)

  - Write the overall equation for the reaction that would occur in mercury oxide cell during discharge.

(2)	Which is better, a silver oxide cell or a mercury oxide cell?	Explain.