Material Selection

Properties of Engineering Materials

Objectives

|  | 1. | To recognise the need of study of engineering materials. |
| --- | --- | --- |
|  | 2. | To classify different types of engineering materials. |
|  | 3. | To identify the properties of engineering materials, with particular to mechanical properties. |
|  | 4. | To identify the properties of ferrous material, non-ferrous material, plastics, ceramics and elastomers. |
| Materials and engineering |  |  |

Chemical, pharmaceutical, manufacturing, fabricating, industrial product, oil and gas, battery and fuel, mining, steel, and energy engineering all involved with materials. Materials also constitute a very important part of our modern day life in many segments such as transportation, housing, clothing, communication, recreation, food production, etc.

All engineers at one time or another will need to select the right material for a design problem. The properties and behaviour of materials must be known. The study of materials aims at:

| 1 | To fulfill the property requirement under the in-service condition, e.g. strength, electrical conductivity under a given range of temperature, etc. |
| --- | --- |
| 2 | To make a trade-off or compromise between conflicting properties, as long as the compromise is acceptable, e.g. a material with high strength may have limited ductility. |
| 3 | To consider the longer term deterioration of material properties that may occur during service operation by corrosion, exposure to heat or UV light radiation, etc. |
| 4 | To consider the cost, including the manufacturing processes the material has to go through to become a finished product. |
| 5 | and more....... |

Classification of materials

Most solid materials can be grouped into three basic classifications: metals, ceramics and polymers. This scheme is based primarily on chemical makeup and atomic structure. In addition there are two other groups of important engineering materials: composites and semiconductors.

| Select a group |  | metals | ceramics | polymers |
| --- | --- | --- | --- | --- |
|  |  | composites | semiconductor |  |
|  | Metallic materials are normally combination of metallic elements. Metals usually have a large number of non-localized electrons, i.e. electrons not bound to any particular atoms. Many special properties of metals are explained by these electrons. Metals are not transparent to visible light and has a lustrous appearance. Metals are strong, yet deformable. In general, metals can be categorized into ferrous and non-ferrous metals. |  |  |  |
|  | Metallic materials are normally combination of metallic elements. Metals usually have a large number of non-localized electrons, i.e. electrons not bound to any particular atoms. Many special properties of metals are explained by these electrons. Metals are not transparent to visible light and has a lustrous appearance. Metals are strong, yet deformable. In general, metals can be categorized into ferrous and non-ferrous metals. |  |  |  |
|  | Polymers include the familiar plastic and rubber materials. Many of them are organic compounds that are chemically based on carbon, hydrogen and other non-metallic elements. They have very large molecular structures, low densities and may be extremely flexible. |  |  |  |
|  | Composites are materials that consist of more than one material type. For example, fiberglass consists of glass fibers embedded within a polymeric material. A composite is designed to display a combination of the best characteristics of each of the component materials. Fiberglass acquires strength from the glass and flexibility from the polymer. |  |  |  |
|  | Semiconductors have electrical properties that are intermediate between the electrical conductors and insulators. Their electrical characteristics are extremely sensitive to the presence of very small amount of concentrations of impurity atoms. The concentration of these impurity atoms can be controlled over a small spatial regions to affect the electrical characteristics. The semiconductors have made possible the advent of integrated circuitry that has totally revolutionized the electronics and computer industries over the last two decades. |  |  |  |

Materials and properties

The important properties of solid materials may be grouped into six different categories:

| Select a category | mechanical | electrical | magnetic |
| --- | --- | --- | --- |
|  | thermal | optical | chemical |

The mechanical properties of a material are concerned with the effects of stress on the material. Different material react differently when a stress is applied to it. - It may change its shape permanently, e.g. bending a copper sheet. - It may break into pieces, e.g. hitting a wine glass. - It may not change its shape at all, .e.g. pulling a steel block with two hands. - It may change its shape but regain its original shape when the stress is removed, e.g. stretching a piece of rubber..

| Select a category | mechanical | electrical | magnetic |
| --- | --- | --- | --- |
|  | thermal | optical | chemical |

| Materials can be either a conductor or an insulator of electricity. Within the conductors, different materials may have different degrees of capabilities in conducting electrical current. There is also a class of materials that are between conductors and the insulators: the semiconductors. |  |  |  |
| --- | --- | --- | --- |
| Select a category | mechanical | electrical | magnetic |
|  | thermal | optical | chemical |

| Many materials are ferromagnetic. Some are magnetically soft, i.e. their magnetic domains can be easily re-oriented under the influence of an imposed magnetic field (e.g. the core sheets in transformers or motors). Some are magnetically hard materials and they are difficult to re-magnetize (e.g. permanent magnets). Once magnetized during manufacturing, the magnetic strength remains. Some can magnetize and de-magnetize repeatedly (e.g. magnetic recording or data storage). |  |  |  |
| --- | --- | --- | --- |
| Select a category | mechanical | electrical | magnetic |
|  | thermal | optical | chemical |

| Thermal properties such as the coefficient of expansion, specific heat, and latent heat of fusion and evaporation are important in many engineering design and manufacturing considerations. Thermal conductivity and heat transfer are often important considerations in engineering design in which heat movement can be either promoted or hindered. |  |  |  |
| --- | --- | --- | --- |
| Select a category | mechanical | electrical | magnetic |
|  | thermal | optical | chemical |

Optical properties can be important for technical or aesthetic reasons. Some materials absorb light and are opaque. Some allow light to go through, and are transparent (e.g. amorphous polymers, glasses and ceramics). Some are translucent (partially transparent) which can be the inherent nature of the materials or by manufacturing processes performed on the transparent materials (e.g. cutting a transparent acrylic material).

| Select a category | mechanical | electrical | magnetic |
| --- | --- | --- | --- |
|  | thermal | optical | chemical |

For design considerations, many chemical properties of materials have to be considered in order for the engineering parts to have a long and effective service life: - the original chemical composition of the material - the physical and chemical environments in which the part will be exposed to - the duration of the service life - the changes that can occur during the manufacturing processes to make the part.

Mechanical properties of materials

In the discipline of mechanical and manufacturing engineering, it is most commonly considered the mechanical properties of materials and used for engineering design purposes.

| Elasticity | It is the ability of a material to return to its original shape after being deformed or strained due to stress resulting from the application of forces. Elastic Modulus or Young's Modulus is used to indicate how far a material can be stretched before it is permanently (plastically) deformed. |
| --- | --- |
| Tensile strength | It is also called the Ultimate Tensile Strength (UTS). It is the maximum stress that a material can be stretched in a tensile fashion before catastrophic failure. Although it is still at a distance from breaking (rupture), the material at this stage is practically considered totally damaged. This is a very common and important measurement for the strength of the material. |
| Shearing strength | It is also called the Ultimate Shearing Strength (USS). It is the maximum stress needed to break a material by shearing. |
| Ductility | Ductility is the ability of the material to undergo deformation without fracture. It has a high capability of plastic deformation. |
| Brittleness | Brittleness is the opposite of ductility. A brittle material deforms only elastically. At some critical stress, fracture occurs suddenly. |
| Hardness | It is the resistance of a material to deformation. |
| Toughness | It is the ability of the material to absorb energy. |
| Fatigue resistance | It is a material's resistance to fatigue. A material may fail when it is subject to a cyclic application of stresses for a long time. Although the stresses are much smaller than the UTS to cause damage in one single application, its cumulative effect will cause the material to crack and fail. |
| Creep resistance | When a stress is applied to a material, it will be strained. When the stress is within the material's elastic range, its strain should be constant. But when the stress is constantly present, then the strain may increase over time. This phenomenon is called creep. |

Ferrous metals

| Ferrous metals, which are based on iron-carbon alloys, includes plain carbon steel, alloy steels, stainless steel and cast iron. Steels are typically produced in two ways: by refining iron ore or by recycling scarp steel. The mechanical properties of ferrous metals are sensitive to the content of carbon as well as the concentrations of other alloying elements. |  |
| --- | --- |
| wrought iron |  |

| Composition | Fe (almost pure) |
| --- | --- |
| Elasticity | medium |
| Tensile strength | 340 MPa |
| Ductility | medium - high |
| Hardness | medium |
| Toughness | high |
| Machinability | good |
| Additional properties | malleable; shock resistant; can be bent, forged, hammer-welded |
| Typical uses | chain links, ornamental work, etc. |

low carbon steel

| Composition | up to 0.25% C |
| --- | --- |
| Elasticity | high |
| Tensile strength | 430 - 480 MPa |
| Ductility | medium |
| Hardness | medium |
| Toughness | high |
| Machinability | fair - good |
| Additional properties | most commonly used; cheap; magnetic; can be welded, forged, case-hardened |
| Typical uses | lightly stressed parts, nails, car bodies, chains, rivets, wire, structural parts, etc. |

medium carbon steel

| Composition | 0.25 - 0.6% C |
| --- | --- |
| Elasticity | high - very high |
| Tensile strength | 480 - 620 MPa |
| Ductility | low - medium |
| Hardness | high |
| Toughness | medium |
| Machinability | fair - poor |
| Additional properties | weldable at lower carbon contents; with increased carbon contents brittleness is increased |
| Typical uses | axles, spindles, couplings, shafts, tubes, gears, forgings, rails, hand tools, dies, ropes, keys, etc. |

high carbon steel

| Composition | 0.6 - 1.5% C |
| --- | --- |
| Elasticity | very high - extremely high |
| Tensile strength | 620 - 820 MPa |
| Ductility | low |
| Hardness | very high |
| Toughness | very low |
| Machinability | very poor (anneal) |
| Additional properties | with increased carbon content brittleness is further increased and ductility is decreased |
| Typical uses | hammers, chisels, screws, drills, taps, dies, blades, punches, knives, saws, etc. |

nickel steel

| Composition | 0.1-4% C, 0.04-1.5% Mn, 1-5% Ni |
| --- | --- |
| Elasticity | medium - extremely high |
| Tensile strength | 310 - 700 MPa |
| Ductility | medium |
| Hardness | high |
| Toughness | very high |
| Machinability | poor |
| Additional properties | nickel improves strength and toughness |
| Typical uses | axles, crankshafts, car parts, camshafts, gears, pins, pinions, etc. |

stainless steel

| Composition | 0.05-0.1% C, 0.8-1.5% Mn, 8.5-18% Ni, 12.5-18% Cr |
| --- | --- |
| Elasticity | medium - very high |
| Tensile strength | 650 - 900 MPa |
| Ductility | medium - high |
| Hardness | medium - very high |
| Toughness | medium - low |
| Machinability | good - fair |
| Additional properties | over 12% Cr protects surfaces from corrosion; 18/8 (Cr/Ni) steel is acid resistant |
| Typical uses | chemical plants, kitchen equipment, cutlery, springs, circlips, etc. |

manganese steel

| Composition | 0.35-1.2% C, 1.5-12.5% Mn |
| --- | --- |
| Elasticity | very high |
| Tensile strength | 700 - 850 MPa |
| Ductility | medium - high |
| Hardness | very high |
| Toughness | high |
| Machinability | extremely poor |
| Additional properties | wear resistant; non-magnetic |
| Typical uses | cutting tools, stone-crushing jaws, dredging equipment, press tools, railway crossings, etc. |

heat resisting steel

| Composition | 0.1% C, 1.5% Si, 1% Mn, 19% Cr, 11% Ni |
| --- | --- |
| Elasticity | high |
| Tensile strength | 690 MPa |
| Ductility | high |
| Hardness | medium |
| Toughness | high |
| Machinability | poor |
| Additional properties | resistant to heat and thermal shock; 10000C max. working temperature |
| Typical uses | burner nozzles, components exposed to high temperatures, etc. |

low-alloy nickel-chrome steel

| Composition | 1-5% Ni, 0.6-1.5% Cr |
| --- | --- |
| Elasticity | high - extremely high |
| Tensile strength | 930 - 1500 MPa |
| Ductility | low |
| Hardness | very high |
| Toughness | high |
| Machinability | good |
| Additional properties | with heat treatment, a wide range of properties may be obtained |
| Typical uses | highly stressed parts, connecting rods, shafts, gears, driving shafts, crankshafts, etc. |

grey cast iron

| Composition | approx. 3-4% C, 1.2-2.8% Si, 0.5-1% Mn |
| --- | --- |
| Elasticity | extremely low |
| Tensile strength | 170 - 350 MPa |
| Ductility | approx. zero |
| Hardness | very high |
| Toughness | very low |
| Machinability | good |
| Additional properties | cheap; easily cast; corrosion and wear resistant; strong in compression; damps vibrations; self-lubricating |
| Typical uses | machine frames, pistons, cylinders, pipes, pulleys, gears, slides, etc. |

ductile iron

| Composition | spheroidal-graphite irons, nodular irons |
| --- | --- |
| Elasticity | very high |
| Tensile strength | 370 - 725 MPa |
| Ductility | medium |
| Hardness | very low - high |
| Toughness | medium |
| Machinability | fair - excellent |
| Additional properties | added magnesium reduces graphite flakes to spheroids, increasing ductility, strength and shock resistance |
| Typical uses | machine frames, pump bodies, pipes, crankshafts, hand tools, gears, dies, office equipment, etc. |

malleable iron

| Composition | 2-3% C, 0.1-0.5% P, 0.5-6% S, 1-5% Si, 0.4-21% Ni, 0.1-5% Cr |
| --- | --- |
| Elasticity | medium |
| Tensile strength | 280 - 510 MPa |
| Ductility | very low - low |
| Hardness | medium |
| Toughness | low |
| Machinability | excellent - good |
| Additional properties | increased ductility and malleability; shock and corrosion resistant; not weldable; can be cast and forged |
| Typical uses | brake drums, levers, links, shafts, hinges, spanners, chains, wheels, vice bodies, etc. |

Plastics

Plastic materials are made from light elements, such as carbon, oxygen and nitrogen. The behavioural characteristics of plastics are different from metals and these properties are available through the addition of additives and reinforcements.

| plastics vs metals | 1 | plastic materials are inherently flexible, allowing the design of snap fits and living hinges, which save assembly cost |
| --- | --- | --- |
|  | 2 | injection moulded plastics allow part consolidations that reduce costs |
|  | 3 | plastic materials exhibit a high strength to weight ratio, allowing structures of lighter weight |
|  | 4 | plastic's excellent friction and wear characteristics offer opportunities for self-lubricated busings and bearings |
|  | 5 | plastic's corrosion resistance reduces the need for paints and coatings |
| types of plastics | 1 | thermoplastic material - can be melted and frozen from liquid to solid repeatedly with the application of heat or cold |
|  | 2 | thermosetting material - cannot turn back into liquid once hardened into a solid state; will simply burn or disintegrate at high temperature |
| thermoplastics vs thermosets | 1 | thermosetting materials have superior abrasion resistance (hardness), rigidity, and high maximum service temperature |
|  | 2 | thermosetting materials have lower impact value, and they tend to be brittle and break more easily |
|  | 3 | thermoplastic materials have shorter moulding time cycle, therefore the processing is less costly than for the thermosetting materials |

Thermoplastic materials

Thermoplastic materials are plastics that can be repeatedly softened and moulded by heating, then hardened by cooling. Thermoplastics can be subdivided into crystalline and amorphous materials. Examples of the thermoplastic materials are discussed below:

| crystalline | materials that have a definite melting point at which they go from solid to molten |
| --- | --- |
| amorphous | materials that gradually soften as they get hotter until they melt together |

polypropylene (PP)

| Relative density | 0.9 |
| --- | --- |
| Flammability | slow burning |
| Tensile strength | 30 - 35 MPa |
| Elongation | 50 - 600% |
| Impact value | 1 - 10 J |
| Max working temperature | 1000C |
| Chemical resistance | very good |
| Additional properties | strong; stiff; very light; good temperature resistance and electrical insulation |
| Typical uses | pipes and fittings, bottles, crates, cable insulation, tanks, cabinets for radios, shoe heels, pumps, etc. |

polyethylene (PE)

| Relative density | 0.92 - 0.95 |
| --- | --- |
| Flammability | slow burning |
| Tensile strength | 11 - 31 MPa |
| Elongation | 50 - 800% |
| Impact value | 5 - 15 J |
| Max working temperature | 85 - 1250C |
| Chemical resistance | good |
| Additional properties | tough; dimensionally stable; improves weather resistant with UV filter pigment |
| Typical uses | buckets, food containers, bags, bottles, pipes, electrical insulation, chemical equipment, etc. |

polytetrafluorethylene (PTFE)

| Relative density | 2.13 - 2.19 |
| --- | --- |
| Flammability | non-flammable |
| Tensile strength | 17 - 25 MPa |
| Elongation | 200 - 600% |
| Impact value | 3 - 5 J |
| Max working temperature | 2600C |
| Chemical resistance | excellent |
| Additional properties | low coefficient of friction; tough; heat resistant; weather and corrosion resistant; can be machined |
| Typical uses | bearings, gaskets, valves, chemical plants, electrical-insulation tapes, non-stick coatings for frying pans, etc. |

nylon 66

| Relative density | 1.14 |
| --- | --- |
| Flammability | self-extinguishing |
| Tensile strength | 70 MPa |
| Elongation | 60 - 300% |
| Impact value | 1.5 - 15 J |
| Max working temperature | 1200C |
| Chemical resistance | good |
| Additional properties | strong; stiff; tough; abrasion resistant; high degree of rigidity; low-friction property |
| Typical uses | bearings, gears, cams, pulleys, combs, bristles for brushes, ropes, fishing lines, raincoats, containers, etc. |

acetal polyoxymethylene copolymer (POM)

| Relative density | 1.41 |
| --- | --- |
| Flammability | self-extinguishing |
| Tensile strength | 60 - 70 MPa |
| Elongation | 65% |
| Impact value | 0.5 - 2 J |
| Max working temperature | 1000C |
| Chemical resistance | good |
| Additional properties | strong; creep resistant; fatigue endurance; dimensionally stable; good electrical insulation; |
| Typical uses | plumbing fittings, bearings, gears, cams, valves, counters, pump parts, etc. |

polystyrene (PS)

| Relative density | 1.05 - 1.08 |
| --- | --- |
| Flammability | slow burning |
| Tensile strength | 50 MPa |
| Elongation | 1 - 35% |
| Impact value | 0.25 - 2.5 J |
| Max working temperature | 1000C |
| Chemical resistance | good |
| Additional properties | rather brittle; transparent; toughening with rubber improves impact and heat resistance |
| Typical uses | vending machine cups, housings for cleaners and cameras, radio cabinets, furniture, toys, etc. |

polyvinyl chloride (rigid PVC, plasticized PVC)

| Relative density | 1.34 - 1.40 |
| --- | --- |
| Flammability | self-extinguishing |
| Tensile strength | 50 MPa |
| Elongation | 10 - 380% |
| Impact value | 1.5 - 18 J |
| Max working temperature | 70 - 1050C |
| Chemical resistance | good |
| Additional properties | rigid PVC is hard, tough, strong, stiff, abrasion resistant; plasticized PVC is more flexible |
| Typical uses | pipes, bottles, chemical plant, lighting fittings, curtain rails, cable covers, toys, balls, gloves, etc. |

polymethylmethacrylate (perspex, PMMA)

| Relative density | 1.19 |
| --- | --- |
| Flammability | slow burning |
| Tensile strength | 55 - 80 MPa |
| Elongation | 3 - 8% |
| Impact value | 0.5 - 0.7 J |
| Max working temperature | 950C |
| Chemical resistance | good |
| Additional properties | completely transparent; strong; stiff; shatter and weather resistant; will not discolour; can be decorated |
| Typical uses | lenses, aircraft glazing windows, roof lighting, sinks, baths, knobs, telephones, dentures, machine guards, etc. |

acrylonitrile-butadiene-styrene (ABS)

| Relative density | 1.1 |
| --- | --- |
| Flammability | self-extinguishing |
| Tensile strength | 30 - 35 MPa |
| Elongation | 10 - 40% |
| Impact value | 7 - 12 J |
| Max working temperature | 1000C |
| Chemical resistance | very good |
| Additional properties | tough; strong; dimensionally stable; good electrical insulation property; can be machined and fabricated |
| Typical uses | television and radio cabinets, motor vehicle radiator grills and panels, battery cases, safety helmets, pipes, water pump and refrigerator parts, etc. |

polycarbonate (PC)

| Relative density | 1.2 |
| --- | --- |
| Flammability | slow burning to self-extinguishing |
| Tensile strength | 60 - 70 MPa |
| Elongation | 60 - 100% |
| Impact value | 10 - 20 J |
| Max working temperature | 1300C |
| Chemical resistance | good |
| Additional properties | strong; tough; high scratch resistance; dimensionally stable; good electrical insulation and optical properties, can be machined and fabricated |
| Typical uses | electrical insulators, capacitor dielectrics, lightweight, 'unbreakable' spectacle lenses, aircraft components and windows, vehicle components, etc. |

Thermosetting materials

Thermosetting materials are plastics that undergo a chemical change when moulded: they become permanently rigid and incapable of being softened again. Thermosetting materials are stronger, more rigid and more brittle than thermoplastics. Examples of the thermoplastic materials are discussed below:

phenol formaldehyde (PF)

| Relative density | 1.35 - 1.5 |
| --- | --- |
| Flammability | very slow burning |
| Tensile strength | 50 - 60 MPa |
| Elongation | 0 - 1% |
| Impact value | 0.5 - 1.5 J |
| Max working temperature | 75 - 1200C |
| Chemical resistance | very good |
| Additional properties | brittle; heavy; hard; rigid; dark coloured; darken under influence of light; very popular thermoset |
| Typical uses | vacuum cleaners, ash trays, buttons, cameras, electrical equipment, dies, handles, gears, costume jewellery, etc. |

urea formaldehyde (UF)

| Relative density | 1.4 - 1.55 |
| --- | --- |
| Flammability | very slow burning to non-flammable |
| Tensile strength | 50 - 75 MPa |
| Elongation | 0 - 1% |
| Impact value | 0.3 - 0.5 J |
| Max working temperature | 750C |
| Chemical resistance | good |
| Additional properties | hard; brittle; rigid; scratch resistant; good electrical insulation property; good colour stability |
| Typical uses | domestic electrical equipment (plugs, sockets and switches), domestic utensils and toys, building panels, etc. |

melamine formaldehyde (MF)

| Relative density | 1.4 - 1.55 |
| --- | --- |
| Flammability | very slow burning to non-flammable |
| Tensile strength | 56 - 80 MPa |
| Elongation | 0 - 0.7% |
| Impact value | 0.2 - 0.5 J |
| Max working temperature | 1000C |
| Chemical resistance | good |
| Additional properties | hard; brittle; rigid; scratch resistant; good electrical insulation property; good colour stability |
| Typical uses | domestic electrical equipment (plugs, sockets and switches), domestic utensils and toys, building panels, etc. |

epoxy resins

| Relative density | 1.12 - 1.19 |
| --- | --- |
| Flammability | slow burning to self-extinguishing |
| Tensile strength | 55 - 60 MPa |
| Elongation | 5 - 10% |
| Impact value | 0.5 - 1.5 J |
| Max working temperature | 170 - 2000C |
| Chemical resistance | good |
| Additional properties | due to many constituents, epoxy resins can be liquids, solutions, pastes or solids; when bonding with glass fibre fillers, they are resistant to water and most reagents; excellent electrical insulation properties |
| Typical uses | adhesive, surface coatings, flooring, electrical insulation, glass-fibre laminates, furniture, etc. |

unsaturated polyester (UP)

| Relative density | 1.12 |
| --- | --- |
| Flammability | slow burning to self-extinguishing |
| Tensile strength | 55 MPa |
| Elongation | 2% |
| Impact value | 0.5 - 1 J |
| Max working temperature | 2000C |
| Chemical resistance | fair |
| Additional properties | good impact resistance and surface hardness; strong when reinforced with glass fibre; |
| Typical uses | domestic baths, boat hulls, car bodies, etc. |

Elastomers

Elastomers refer to ductile, tough polymers that frequently have high elasticity. Natural rubber is an obvious and very important elastomer. Most elastomers are formulated to meet a specific property requirement found lacking in natural rubber. Because most elastomers lend themselves to being compounded with many different materials, the choice of elastomers compounds available and the range of their uses is unlimited. Examples of the elastomers are discussed below:

natural rubber (polyisoprene)

| Elongation | excellent |
| --- | --- |
| Heat aging | good |
| Flame resistance | poor |
| Tear resistance | good |
| Abrasion resistance | excellent |
| Compression set resistance | good |
| Chemical resistance | poor to fair |
| Freedom from odour | excellent |
| Max working temperature | 1000C |
| Typical uses | vehicle tyres (modified by additives and vulcanization) |

nitrile rubber

| Elongation | good |
| --- | --- |
| Heat aging | excellent |
| Flame resistance | poor |
| Tear resistance | fair |
| Abrasion resistance | good |
| Compression set resistance | good |
| Chemical resistance | excellent |
| Freedom from odour | fair |
| Max working temperature | 1300C |
| Typical uses | petrol and fuel oil hoses, hose linings, aircraft fuel tank linings, etc. |

silicone rubber

| Elongation | fair |
| --- | --- |
| Heat aging | excellent |
| Flame resistance | fair |
| Tear resistance | poor |
| Abrasion resistance | poor |
| Compression set resistance | fair |
| Chemical resistance | poor to fair |
| Freedom from odour | fair |
| Max working temperature | 2900C |
| Typical uses | space vehicles, artificial satellites, etc. |

butyl rubber

| Elongation | fair |
| --- | --- |
| Heat aging | excellent |
| Flame resistance | poor |
| Tear resistance | good |
| Abrasion resistance | good |
| Compression set resistance | fair |
| Chemical resistance | poor |
| Freedom from odour | good |
| Max working temperature | 1200C |
| Typical uses | hose linings, construction industry sealant, etc. |

polyurethane rubber

| Elongation | fair |
| --- | --- |
| Heat aging | good |
| Flame resistance | excellent |
| Tear resistance | excellent |
| Abrasion resistance | excellent |
| Compression set resistance | good |
| Chemical resistance | good |
| Freedom from odour | excellent |
| Max working temperature | 1200C |
| Typical uses | shoe heels, painting rollers, mallet heads, oil seals, diaphragms, anti-vibration mountings, gears, pump impellers, cushion tyres, etc. |

polychloroprene rubber (neoprene)

| Elongation | excellent |
| --- | --- |
| Heat aging | very good |
| Flame resistance | good |
| Tear resistance | good |
| Abrasion resistance | excellent |
| Compression set resistance | fair |
| Chemical resistance | good |
| Freedom from odour | good |
| Max working temperature | 1300C |
| Typical uses | electrical insulators, gaskets, hoses, engine mounts, sealants, rubber cements, protective clothing, etc. |

Ceramics

Ceramics are inorganic, non-metallic materials, which are processed and may be used at high temperatures. They consist mainly of silicon chemically combined with non-metallic elements such as oxygen, carbon and nitrogen and with metallic compounds.

| General properties | 1 | generally hard and brittle, does not readily deform plastically |
| --- | --- | --- |
|  | 2 | high electrical resistance |
|  | 3 | high melting temperatures |
|  | 4 | low electrical and thermal conductivity |
|  | 5 | high compressive strengths |
|  | 6 | chemically inert |
|  | 7 | can be optically opaque, semi-transparent, or transparent |
| Type 1: Crystalline ceramics | 1 | composed mainly of silicon and oxygen |
|  | 2 | uses: whiteware, e.g. pottery structural clay products, e.g. brick, tile, terracotta, etc, refractory, e.g. high temperature resistant products, crucible, etc. Portland cement abrasives, e.g. grinding wheels |
| Type 2: Glasses | 1 | silicon oxide based composition |
|  | 2 | uses: borosilicate glass, e.g. cookware, window glasses, etc. E-glass (electrical-grade glass), e.g. fibre reinforcing component in composites enamels, e.g. glass coatings applied to metals |
| Type 3: Glass ceramics | 1 | initially shaped as a glass, then heat treated to crystallize over 90% |
|  | 2 | special properties: good resistance to thermal shock strength is greater than traditional glasses |
|  | 3 | uses: cooking utensils, e.g. Corning ware medical, e.g. dental restoration engineering, e.g. space vehicles, electronic, etc. |

Tutorial

|  | The 13A plug is one of the most common electrical components we use. It contains numerous parts and together with the cable and socket, it is an essential part of almost every household electrical device. The various parts of a 13A plug are categorized below. Identify the material of construction for the different parts of the plug. |  |  |  |
| --- | --- | --- | --- | --- |
| Parts of 13A plug |  |  |  |  |
| good conductors |  | good insulators | associative parts |  |